# Bio-coating Governs Systemic Uptake of Oral Polymeric Nanoparticles

# Layman's Abstract

When medications are packaged inside tiny particles and swallowed, they must cross a sticky mucus layer, pass through the intestinal lining, and enter the bloodstream before they can work. We discovered that particles with the right surface coating can reach the bloodstream at remarkably high levels — up to 45% of the dose — through the ordinary cells lining the intestine. This project will determine which coatings work best at each barrier and build the first set of rules for designing effective swallowable nanoparticle therapies.

# PROJECT SUMMARY

How do surface coatings govern the fate of oral nanoparticles across mucus diffusion, enterocyte processing, and systemic absorption? Oral NP therapies promise to transform treatment of chronic diseases, yet sequential gastrointestinal (GI) barriers — mucus, epithelium, and post-epithelial clearance — have been studied in isolation, leaving no mechanistic understanding of how coating properties govern particle fate across these sequential stages. The prevailing strategy of PEG-coating for mucus penetration faces a fundamental dilemma: improved mucus transport does not guarantee epithelial transcytosis, and efficient cellular uptake does not ensure basolateral release. We propose to define NP coating strategies that synchronously optimize mucus navigation, enterocyte trafficking, and transepithelial passage, and to validate a workflow that connects in vitro indices to systemic uptake. Our central hypothesis is that GI uptake is maximized by coatings that both improve mucus mobility and bias enterocyte processing toward productive transcytosis rather than apical trapping or intracellular sequestration. Our preliminary data strongly support this: intact polystyrene NPs achieve 45% systemic uptake via isolated intestinal loop and 35% via oral gavage, PLA NPs reach ~30%, and NP-encapsulated vedolizumab delivered 73% bioavailability relative to subcutaneous injection — with uptake occurring in the jejunum via enterocytes, not M-cells. Using PS/PCRed and PLA NPs (450 and 1000 nm) coated with mucin or PEG at varying molecular weights (1.5–300 kDa), we will: (1) quantify how coatings modulate enterocyte processing and transepithelial passage using a 96-hour Caco-2 platform with dual mucus models; (2) build a coating-dependent mucus mobility and interaction matrix via confocal particle tracking; and (3) validate the framework in vivo using isolated intestinal loop and oral gavage in rats. Successful completion will yield the first mechanistic framework connecting NP coating properties to systemic bioavailability, accelerate development of oral biologics, and — because the framework uses non-degradable polystyrene as a core tracer — directly inform understanding of how environmental micro/nanoplastics traverse identical GI barriers to reach systemic organs.

SPECIFIC AIMS AND HYPOTHESIS: Oral nanoparticle (NP) therapies promise to transform treatment of chronic diseases, yet their development is hampered by sequential gastrointestinal (GI) barriers — luminal mucus, the epithelial brush border and glycocalyx, polarized intracellular trafficking, and post-epithelial clearance. Current approaches study these barriers in isolation, and the prevailing strategy of PEG-coating for mucus penetration faces a fundamental dilemma: improved mucus transport does not guarantee epithelial transcytosis, and efficient cellular uptake does not ensure basolateral release. The most rigorous pharmacokinetic studies show that absolute oral bioavailability of intact PEG-coated particles remains below 0.1%. Moreover, most current strategies target M-cells in Peyer’s patches, yet these represent less than 1% of the intestinal epithelium; our data show that the dominant uptake pathway is through enterocytes in the jejunum, a Peyer’s patch–poor region — opening a far larger absorptive surface than the field has considered. No quantitative framework currently links mucus mobility, enterocyte processing, and transepithelial passage to predict systemic exposure of intact particles.

Our long-term goal is to establish design principles enabling predictable, efficient oral delivery of intact NPs. The objective of this application is to define NP coating strategies that synchronously optimize mucus navigation, enterocyte trafficking, and transepithelial passage, and to validate a workflow that predicts systemic uptake. Our central hypothesis is that GI uptake is maximized by coatings that perform dual functions: (i) they create a biomolecular corona that improves mucus mobility and epithelial access, and (ii) they bias enterocyte processing toward productive transcytosis rather than apical trapping or intracellular sequestration — with the rate-limiting step being the subset of trafficking events terminating in basolateral delivery. This hypothesis is supported by our preliminary data: intact polystyrene (PS) NPs achieve 45% systemic uptake via isolated intestinal loop and 35% via oral gavage [14, 16], poly(lactic acid) (PLA) NPs reach ~30% [14, 15], and NP-encapsulated vedolizumab delivered 73% bioavailability relative to subcutaneous injection [17, 32]. Critically, confocal imaging confirmed that the majority of uptake occurs in the jejunum via enterocytes, not M-cells [14, 16] — redirecting the mechanistic focus of this proposal toward enterocyte-mediated transcytosis and justifying the Caco-2 platform as our primary in vitro model.

To test this hypothesis, we propose the following Specific Aims using PS/PCRed and PLA NPs (450 nm and 1000 nm) coated with mucin or PEG at varying molecular weights (1.5–300 kDa):

Aim 1: Define how coatings modulate enterocyte processing and transepithelial passage using a 96-hour Caco-2 platform. We will quantify apical adhesion, intracellular internalization, and basolateral transcytosis using polarized Caco-2 Transwells with confocal z-stack analysis over 0.5–96 h, with mucus modeled via commercial mucin overlays and Caco-2/HT29-MTX co-cultures. Expected outcome: Coatings that maximize the transcytosis index, revealing the B(+/−) paradox (high uptake ≠ high transcytosis) in the 72–96 h window.

Aim 2: Build a coating-dependent mucus mobility and interaction matrix. Using porcine gastric mucin gels at 3% and 5% (w/w), we will quantify diffusion coefficients and interaction profiles (free diffusion, reversible binding, irreversible trapping) via confocal particle tracking and ZetaView analysis. Integration with Aim 1’s transcytosis indices will identify coatings that optimize both mucus transit and epithelial transport. Expected outcome: A diffusion–interaction matrix identifying formulations with ≥5-fold enhanced mucus transport that correlate with productive transcytosis.

Aim 3: Validate the predictive framework in vivo using isolated intestinal loop and oral gavage. Top-performing formulations from Aims 1 and 2 will be tested in a rat isolated loop model (±precoating × ±native mucus), mapping in vitro indices to absolute bioavailability. Top formulations advance to oral gavage to test predictions under full GI transit complexity. Expected outcome: A validated quantitative relationship between in vitro indices and in vivo systemic uptake — the first predictive design framework for oral NP bioavailability.

Impact: This proposal replaces the empirical screen-and-hope approach dominating oral NP development with mechanism-guided design rules linking NP properties to systemic bioavailability. The framework — built using non-degradable PS as a core tracer — also directly informs understanding of how environmental micro/nanoplastics traverse identical GI barriers to reach systemic organs.

RESPONSE TO REVIEWERS

Why does it matter whether we can connect a nanoparticle’s surface coating to its systemic fate after oral administration? The answer extends beyond drug delivery. Humans ingest an estimated 5 grams of microplastic per week — roughly a credit card’s worth — yet the mechanisms by which these particles cross the intestinal epithelium and accumulate in systemic organs remain unknown. Our preliminary data, showing that intact polystyrene nanoparticles achieve 45% systemic uptake through enterocytes in the jejunum (not M-cells in Peyer’s patches), demonstrate that particle surface properties govern transit through each sequential GI barrier. A mechanistic framework connecting coating properties to mucus diffusion, enterocyte processing, and transepithelial passage would both accelerate rational design of oral nanotherapeutics and provide the first mechanistic basis for understanding how environmental particulates reach human tissues.

We thank the reviewers for their constructive critique. The resubmission incorporates the following major changes:

Focused scope. The formulation matrix has been narrowed from 200+ combinations to a defined set: PS/PCRed and PLA nanoparticles at 450 nm and 1000 nm, coated with mucin or PEG at molecular weights spanning 1.5–300 kDa. This focused library is justified by our preliminary data, which identify mucin and the PEG 35–200 kDa range as the most informative coating conditions [14–16].

Enterocyte-dominant uptake pathway. Confocal imaging confirms that NP absorption occurs in the jejunum via enterocytes, not M-cells [14, 16] — validating Caco-2 as the mechanistically appropriate in vitro platform. To address mucus model concerns, we now employ a dual strategy: commercial mucin overlays for reproducibility and Caco-2/HT29-MTX co-cultures for physiological relevance.

PEG dilemma addressed. We explicitly confront the disconnect between mucus penetration and systemic uptake: the most rigorous PEG studies show <0.1% oral bioavailability for intact particles [58]. This motivates studying barriers both independently (to identify rate-limiting steps) and in combination (co-culture validation), resolving the concern about separate vs. integrated barrier assessment.

In vivo validation strengthened. Aim 3 now includes oral gavage as a confirmatory step following isolated loop experiments, directly addressing reviewer concerns about clinical relevance. Animal numbers are reduced to 240 with formal power analysis (n=6, ≥88% power for primary comparisons). Blood draw volumes, anesthesia protocols, and humane endpoints are fully specified.

Innovation reframed. We now lead with four findings that existing approaches cannot explain: 45% systemic uptake of intact particles, the B(+/−) paradox (high cellular uptake ≠ high transcytosis), the 72–96 h diagnostic window, and Caco-2 predictive validation for in vivo rankings. Vedolizumab pilot data (73% bioavailability vs. subcutaneous injection) are presented as preliminary data supporting the platform’s translational potential. Rather than the sequential barrier optimization that reviewers noted as a limitation of prior work, we now evaluate all formulations across mucus diffusion, epithelial transcytosis, and in vivo uptake in parallel, capturing trade-offs that sequential screening would miss.

# Research Strategy:

## I. Significance:

Biologics and therapeutics have revolutionized the pharmaceutical landscape due to their high specificity, potency, and functional diversity, yet they remain susceptible to chemical and enzymatic degradation [1]. These vulnerabilities, coupled with limited permeability across the mucosal layer and intestinal epithelium, severely restrict oral bioavailability [2], and the large size and charge of these molecules often prevent them from reaching intracellular targets [3]. NPs offer a promising solution for oral delivery of these proteins. Our lab has an extensive history of encapsulating proteins in small, active NPs [4-9] and developing effective release rates. Until recently, oral bioavailability remained low, but in a recent study we achieved a relative bioavailability of 70%, compared to subcutaneous injection using isolated loop experiments. Building on that result, this project will advance intracellular delivery and transcytosis through coated-particle/cell-culture interaction studies (Aim 1), enhance mucosal penetration by characterizing in vitro diffusion of coated NPs and the role of surface coatings in barrier passage (Aim 2), and improve systemic uptake and drug bioavailability through isolated loop experiments informed by the earlier Aims (Aim 3). The resulting data will support a predictive model for evaluating NP efficacy for oral delivery.

The therapeutic value of an oral nanoparticle formulation ultimately depends on systemic uptake, yet current development remains empirical because no validated framework connects a particle’s physicochemical properties and surface coatings to its fate across the sequential stages of GI transit — mucus diffusion, epithelial transcytosis, and systemic absorption. A formulation that performs well at one stage may fail at another — strong mucus penetration does not guarantee epithelial transcytosis, and efficient cellular uptake does not ensure basolateral release. Establishing a predictive model that links measurable in vitro transport indices to in vivo systemic exposure would enable rational selection of NP designs and coatings most likely to achieve oral bioavailability, shifting the field from empirical screening to mechanism-guided design.

This research is significant because it challenges existing paradigms [13] and seeks to provide a comprehensive, predictive framework for oral NP design. Preliminary data from the applicants has already demonstrated unprecedented systemic uptake (up to 45% for polystyrene and 30% for PLA NPs) and a 10-fold enhancement with bio adhesive precoating’s [14-17] directly contradicting the prevailing notion about surface charge. By systematically investigating how NP coatings can be engineered to concurrently optimize mucus penetration and promote specific cellular trafficking pathways for transepithelial passage, this work promises to dramatically improve the efficacy of orally administered nanomedicines. The development of a comprehensive property-function matrix correlating NP physicochemical properties with mucus diffusion, transcytosis efficiency, and ultimately in vivo systemic uptake will be a substantial advancement. This will lead to the identification of lead candidates with significantly enhanced (potentially >10-fold) transepithelial delivery and provide a foundational dataset for predictive modeling, ultimately accelerating the translation of promising nanotherapeutics by overcoming the critical hurdle of efficient oral bioavailability

Identifying the optimal coating is not an academic exercise — it has immediate translational relevance. Our laboratory has established, through prior funding, bioerodible nanoparticle delivery systems that achieve high protein loading with controlled release and minimal burst — a critical requirement for protein therapeutics that are sensitive to dose dumping and degradation. However, formulation optimization for loading and release kinetics does not guarantee a surface chemistry conducive to mucosal diffusion or epithelial transport. The particle surface that emerges from an optimized encapsulation process may trap in mucus or fail to engage productive transcytosis pathways, regardless of how well the core performs. What remains is identifying a coating — whether a natural material such as mucin or a synthetic polymer such as PEG — that enhances both mucus diffusion and epithelial transport without compromising the controlled release properties of the underlying particle. This challenge is shared by every laboratory developing oral nanoparticle systems: a predictive framework that links coating properties to mucosal and epithelial fate would enable rational surface modification matched to any formulation, replacing empirical screening of coating-particle combinations with mechanism-guided design.

Beyond drug delivery, the predictive framework developed here has direct relevance to an emerging public health concern: the accumulation of micro- and nanoplastic particles in human tissues. Recent studies have documented plastic polymers in prostate, breast, lung, and colorectal cancer specimens [61], yet the mechanisms by which ingested particles cross the intestinal epithelium and reach systemic organs remain poorly understood. The oral route is a primary pathway for human microplastic exposure, and the sequential barriers these particles must navigate—mucus diffusion, epithelial transcytosis, and systemic distribution—are identical to those studied in this proposal. The mechanistic indices and in vitro–to–in vivo mapping tools developed here, built using non-degradable polystyrene as a core tracer, are directly applicable to understanding how environmental particulates traverse the same gastrointestinal stages, potentially informing risk assessment for unintentional particle exposure.

## II. Innovation

Our preliminary data reveal phenomena that the field’s current approaches cannot explain — and this proposal builds the framework to decode them. Existing studies of oral nanoparticle transport treat mucus diffusion, cellular uptake, and systemic absorption as independent variables, measured in isolation with different particle systems, cell lines, and animal models. This fragmented approach has produced a familiar but misleading narrative: optimize mucus penetration, and systemic delivery will follow. Our data expose findings that directly contradict this assumption and that no single-stage study could have predicted:

First, intact polystyrene and PLA nanoparticles achieve 45% and 30% systemic uptake, respectively — orders of magnitude above the <1% typically reported for oral particles [14–17]. This result cannot be explained by diffusion data or transcytosis assays alone; it reflects a multi-stage process that must be studied as such. Second, coatings that maximize cellular internalization do not maximize transcytosis — the “B(+/–) paradox” we identified, in which PEG100 kDa drives ~83% cellular uptake but <2% basolateral transport, while PEG35 kDa achieves a 22-fold higher transcytosis efficiency ratio. This paradox is invisible to any study that equates “uptake” with “delivery.” Third, the most diagnostically informative transport occurs between 72 and 96 hours — a time window that the vast majority of published Caco-2 studies never reach, meaning the critical biology of productive transcytosis has been systematically missed. Fourth, mucin-coated polystyrene particles tested in our Caco-2 Transwell system produce transcytosis rankings that correspond to their in vivo systemic uptake — establishing that the Caco-2 platform under our experimental conditions has genuine predictive power for oral bioavailability of intact particles, not merely descriptive value for cellular uptake.

These findings motivate three methodological innovations embedded in this proposal. (1) Synchronous rather than sequential optimization. Rather than filtering candidates through mucus penetration first and transcytosis second, we analyze the full formulation library for both properties in parallel (Aim 1 and Aim 2), generating a complete property–function matrix that captures trade-offs — such as the PEG dilemma — that sequential screening would obscure. (2) Intact particle tracking with non-leaching systems. By using fluorescent polystyrene and covalently labeled PLA as core particles, we eliminate the pervasive confound of dye leakage that has inflated oral NP uptake estimates throughout the literature, ensuring that what we measure as “systemic exposure” is genuinely particle-associated. (3) Quantitative in vitro–to–in vivo mapping. The isolated intestinal loop (Aim 3) enables absolute bioavailability determination under controlled conditions, allowing us to map transcytosis indices and mucus mobility scores directly to systemic outcomes — converting mechanistic measurements into predictive tools rather than descriptive correlations.

Together, these innovations replace the empirical screen-and-hope workflow that currently dominates oral nanoparticle development with a mechanism-guided design framework: one that explains why certain coatings succeed across all stages of GI transit, not merely whether they do at any single stage.

## III. Approach:

Our design systematically isolates key variables in NP transport to avoid confounded results. We achieve this by separately analyzing epithelial cell interactions (Aim 1, studying surface chemistry’s effect on uptake with/without mucus) and how the same formulations navigate the mucus barrier (Aim 2, free from cellular confounders). This allows us to distinguish their specific contributions, conducting in vivo studies using a live-rat isolated intestinal loop (Aim 3). This integrates the phenomena while removing interference from gastric or colonic variables, thereby focusing solely on intestinal transport mechanisms. The loop’s jejunal targeting matches the tissue compartment where our preliminary data show uptake occurs, and its controlled geometry enables the quantitative in vitro–to–in vivo comparison that is the central objective of this proposal. We employ a proven, burst-free drug release platform, ensuring that observed changes in systemic exposure accurately reflect transport phenomena, not artifacts from drug release. As a final confirmatory step, the top-performing formulations identified through the isolated loop studies will be evaluated by oral gavage to test whether the predictive framework retains validity under the full complexity of GI transit, including gastric acid, bile exposure, and variable regional residence times (Activity 4).

Aim 1: Cellular Model to Determine NP Uptake, Transcytosis, and Localization: The primary objective of this Aim is to systematically determine how NP physicochemical properties, and a targeted library of surface coatings influence their cellular uptake efficiency, mechanisms of transepithelial transport, and ultimate intracellular fate using established intestinal epithelial cell culture models (Caco-2 monocultures and Caco-2/HT29-MTX co-cultures incorporating mucus-secreting goblet cells). This Aim will be conducted in concert with mucus diffusion studies (Aim 2) to build an integrated understanding of NP behavior across sequential GI barriers, rather than filtering candidates based on a single barrier performance. To dissect the independent and combined contributions of NP coating and the mucosal environment, we employ a four-condition experimental framework: coated NPs with an apical mucus layer (Condition A), coated NPs without mucus (Condition B), uncoated NPs with a mucin overlay (Condition C), and uncoated NPs without mucin (Condition D). This design allows us to isolate coating-driven effects from mucus-mediated modulation of intracellular trafficking and to identify conditions under which the mucus layer functions not as a passive barrier but as an active facilitator of productive transcytotic transport. We hypothesize that optimal NP transcytosis across intestinal epithelium is governed by a synergistic interplay between NP coating properties and the presence of an apical mucus layer, which collectively dictate entry into and navigation through productive intracellular trafficking pathways, and that by systematically evaluating a comprehensive library of NPs for both cellular processing (this Aim) and mucus diffusion (Aim 2) in parallel, we can deconstruct the specific NP design rules governing success at each sequential barrier (see Preliminary Studies below). This Aim will specifically test how NP formulations, varying in core properties and coatings, influence internalization routes, trafficking pathways (transcytotic vs. lysosomal/recycling), and the ultimate efficiency of transepithelial passage in Caco-2 monolayers.

Our in vivo data demonstrate that intact nanoparticle uptake occurs predominantly in the jejunum—a Peyer’s patch–poor region where absorptive enterocytes, not M-cells, are the dominant epithelial population. Confocal imaging of intact tissue confirms particle localization within enterocyte cytoplasm and at the basolateral membrane, with subsequent detection in blood and systemic organs within approximately 3 hours. These findings directly implicate absorptive enterocytes as the primary cellular gateway for transepithelial passage in our system, making the Caco-2 Transwell model—which recapitulates enterocyte polarization, brush border architecture, tight junction regulation, and directional vesicular trafficking—the most mechanistically appropriate in vitro platform for this investigation.

To address the recognized limitation that standard Caco-2 monocultures lack a mucus layer, we employ a complementary dual-model strategy. First, we apply a defined commercial mucin layer atop Caco-2 monolayers, providing a reproducible and compositionally controlled mucus constraint that enables systematic comparison of coating effects across the full nanoparticle library under identical conditions. Second, we use Caco-2/HT29-MTX co-cultures in which goblet cells secrete an endogenous mucus layer, providing a more physiologically representative barrier that captures the heterogeneity and dynamic turnover of native intestinal mucus. The combination of these two approaches ensures both experimental rigor—through the reproducibility of the defined mucin system—and physiological relevance—through the biological complexity of the co-culture model. Concordance between the two systems strengthens confidence in formulation rankings; discordance identifies coatings whose performance depends on mucus composition or turnover, directly informing which in vitro conditions best predict in vivo outcomes.

## Justification and Feasibility

Oral delivery of nanotherapeutics remains a formidable challenge due to the complex, sequential barriers of the GI tract, primarily the mucus layer and the intestinal epithelium. While NP properties like size, charge, and hydrophobicity are known to influence interactions with these barriers, a unified understanding of how these factors collectively govern the journey from lumen to systemic circulation is lacking. Current approaches often study these barriers in isolation or rely on sequential optimization, which may prematurely discard promising candidates. Our strategy, by evaluating cellular transport (Aim 1) in parallel with mucus diffusion (Aim 2) for a broad range of NPs, addresses this critical gap.

Review of relevant literature: The literature on NP uptake reveals contradictory results, reflecting the difficulty of studying mucus diffusion, cellular uptake, and intracellular routing as interconnected processes rather than isolated variables. Our review highlights three aspects that a single cohesive study must address. First, the GI mucus layer is not merely a passive barrier: NP physicochemical properties such as charge, size, and hydrophilicity dictate aggregation and diffusion rates within the mucus [18], and charged or hydrophobic NPs exhibit strong muco-interactions that shape subsequent epithelial uptake [19, 20]. Because mucus interactions modulate downstream cellular events, studying NP-cell behavior without accounting for the mucus environment can produce misleading conclusions.

Second, high cellular internalization does not reliably predict productive transcytosis. NP hydrophobicity, size, and shape influence uptake [19, 21], yet without an apical mucus layer, heavily internalized particles often fail to reach the basolateral side [22]. This Aim examines how coatings (mucin, PEG series) determine intracellular fate, including the balance between basolateral exocytosis, lysosomal degradation, and apical recycling. Third, intracellular sorting after uptake is itself coating-dependent: NP charge influences interactions with efflux (MDR1/P-gp) and influx (MRP1) transporters, and surface modifications such as mucin coatings redirect trafficking in ways that can offset initial uptake advantages [23, 24]. Designing particles that couple efficient entry with directed transit toward productive exocytosis requires understanding all three barriers in concert.

Preliminary data for Aim 1: We quantified the transcytosis of 0.45 um Cy5-labeled polystyrene nanoparticles bearing eight distinct surface coatings across Caco-2 monolayers under a 2x2 factorial design (coating +/-, mucus +/-; n=3 biological replicates per coating, n=4 for mucin). Particle numbers were estimated from fluorescent area measurements using average particle diameter and 1315.9 fields of view per insert. Under the full condition A(+/+), cumulative 96-hour transcytosis revealed a clear PEG molecular weight optimum spanningthe 35-200 kDa range: PEG200k transported ~41.4 million particles (std 3.36M), followed by PEG100k at ~31.6M (std 6.75M), PEG35k at ~19.5M (std 1.60M), and mucin at ~12.3M (std 1.44M), while PEG20k (7.07M), PEG300k (5.50M, std 3.98M), PEG8k (4.81M), and PEG1.5k (4.48M) showed substantially lower transport. Uncoated controls confirmed that coatings are essential: condition C(-/+) yielded only ~2.84M particles, and condition D(-/-) yielded ~0.068M particles, (condition B) nearly abolished transport for the top-performing coatings — PEG200k dropped from 41.36M to 0.93M particles, a 44-fold reduction, and PEG100k fell from 31.57M to 6.25M, an approximately 5-fold decrease. These results demonstrate that mucus functions not merely as a passive barrier but as an essential modulator of coating-mediated transcytosis (Figure 1).

The relationship between cellular internalization and productive transcytosis further distinguishes high-performing coatings from those that promote intracellular trapping. Uncoated particles without mucus (D(-/-)) exhibited the highest internalization at ~77.6M particles, consistent with non-specific uptake and retention. Among coated formulations, PEG200k under condition A(+/+) internalized only ~4.33M particles (std 0.11M) yet transcytosed ~41.4M, yielding a transcytosis efficiency ratio of 44.15 (per-experiment mean 44.28 +/- 2.56 SEM). PEG35k followed a similar pattern, with ~3.51M internalized and ~19.5M transcytosed (efficiency 25.56; 26.19 +/- 2.47 SEM). By contrast, PEG100k internalized ~36.9M particles (std 43.42M, exceeding the mean) and PEG300k internalized ~39.9M (std 44.51M, also exceeding the mean), yielding markedly lower efficiencies of 3.97 and 0.64, respectively; the extreme variance in these two coatings warrants further mechanistic investigation. This inverse relationship between intracellular retention and productive transcytosis suggests that the most effective coatings promote rapid vesicular transit rather than prolonged cytoplasmic accumulation — a finding consistent with our previous work demonstrating that surface precoating strategies can reduce aggregation and enhance diffusion through the mucus layer [14, 15].

Time-resolved collection revealed that basolateral particle accumulation was minimal during the first 48 hours across all formulations, with dramatic acceleration occurring between 72 and 96 hours for the top-performing coatings. PEG100k transported ~21.6M of its cumulative ~31.6M particles during the final 24-hour collection period (T4), representing approximately 68% of total transport in that terminal window. PEG200k exhibited a similar late-phase surge, with ~22.2M of ~41.4M cumulative particles appearing at T4 (~54% of total). PEG35k likewise showed pronounced late accumulation. These kinetics justify our 96-hour collection protocol and suggest that coating-dependent transcytosis involves a lag phase — potentially reflecting the time required for vesicular processing and basolateral exocytosis. Live/dead viability assays confirmed greater than 95% cell viability throughout the 96-hour experimental window, ruling out paracellular leak as a confound.

Figure 1  - PEG molecular weight modulates nanoparticle transcytosis through intestinal epithelium in a mucus-dependent manner. (A) Cumulative transcytosis at 96 h across PEG coatings, with peak transport at PEG35k–PEG100k in the presence of mucus. (B) Transcytosis efficiency (transcytosis/internalization) by coating. (C) Relationship between internalization and transcytosis across coatings, highlighting the mucus-dependent transport paradox. (D) Internalization and transcytosis responses by coating condition. (E) Time course of cumulative transcytosis under mucus and no-mucus conditions. Data are mean ± SD, n = 3 independent experiments, using 450 nm PS-Cy5 NPs on differentiated Caco-2 monolayers.

### Research Design: Methodology

Activity 1.1 Mucin Labeling: To distinguish coating mucin from the apical mucus layer, we will employ fluorescein-5-thiosemicarbazide (FTSC) labeling following established protocols [25] with optimization as needed. Dried mucin will be dissolved in PBS and dialyzed into sodium carbonate buffer (pH 9.0). A 10 mM FTSC solution in DMSO will be prepared, and mucin and FTSC will be combined at a 1:20 molar ratio for a 2 h reaction at room temperature, protected from light. Excess dye will be removed by dialysis against PBS (pH 7.4) at 4 °C for 48 h. Labeled mucin will be stored at 4 °C for short-term use or −20 °C for long-term storage. This approach preserves O-glycan structures, minimizes alterations to mucin’s biophysical properties, and reduces nonspecific interactions during NP–mucus diffusion and uptake studies.

Activity 1.2 Preparation of Epithelial Cell Model and Experimental Conditions: Caco-2 cells will be seeded at approximately 150 000 cells per Transwell insert (50 000 cells/cm2) and differentiated for 21 days to form tight, polarized monolayers. Our four-condition framework systematically evaluates coating and mucus layer contributions: Condition A (+coating/+mucus) will consist of coated NPs applied onto monolayers overlaid with a defined commercial mucin layer (e.g., porcine gastric mucin) or mucus secreted by an HT29-MTX co-culture; Condition B (+coating/-mucus) will apply coated NPs onto monolayers without mucin; Condition C (-coating/+mucus) will deliver uncoated NPs in the presence of a defined commercial mucin layer (e.g., porcine gastric mucin) or mucus secreted by an HT29-MTX co-culture; and Condition D (-coating/-mucus) will represent uncoated NPs without mucin. Corresponding cell-free controls will distinguish passive diffusion from active cellular transport. Initial coatings will focus on a polyethylene glycol (PEG) series spanning molecular weights from 1.5 kDa to 300 kDa, based on preliminary data that identified an optimum between 35 kDa and 200 kDa for productive transcytosis. We will then extend the PEG molecular weight series beyond the initial optimum, testing 1.5, 5, 10, 20, 35, 50, 100, 200, and 300 kDa to define the full MW-transcytosis relationship, and compare PEG performance against mucin coatings under all four conditions. All NPs (450 nm polystyrene cores) will be conjugated with stable fluorophores (e.g., FITC or rhodamine) to enable quantitative imaging of particle localization.

The 96-hour collection window is supported by our preliminary kinetic data (see Preliminary Studies above), which demonstrate that the most diagnostically informative transcytosis occurs late and that coating-dependent differences become apparent only after 48 hours of incubation. Live/dead viability assays in our laboratory confirm that Caco-2 monolayers maintain >95% viability throughout the full 96-hour protocol, consistent with the well-established capacity of differentiated Caco-2 cultures to sustain barrier function for extended periods.

Activity 1.4 Intracellular localization: To investigate subcellular routing under Condition A, cells will be fixed at 96 h and immunostained for LAMP1 (lysosomal marker), RAB11 (recycling endosome marker), and GM130 (Golgi marker). Confocal colocalization analysis via ImageJ will quantify the percentage of NP signal overlapping each organelle marker. A subset of samples will be processed for TEM to validate trafficking pathways at the ultrastructural level. This concise, hypothesis-driven analysis will reveal how specific coatings (e.g., PEG 35 kDa versus PEG 100 kDa) bias NPs toward recycling versus degradative routes, informing mechanistic insights for subsequent aims.

Based on our preliminary data, we anticipate that under Condition A, PEG200 kDa coatings will yield the highest cumulative basolateral particle counts (~41.4M particles at 96 h), followed by PEG100 kDa (~31.6M) and PEG35 kDa (~19.5M), each substantially exceeding mucin alone (~12.3M particles). We note that PEG100 kDa and PEG300 kDa estimates carry higher inter-replicate variance and will require confirmation across expanded biological replicates. Under Condition B, all coatings will exhibit robust cellular uptake (e.g., ~64.8M internalized particles for PEG100 kDa) yet markedly reduced transcytosis (~6.2M), confirming the "B(+/-) paradox." Efficiency ratios (transcytosis/internalization) are expected to peak for PEG200 kDa (~44x) and PEG35 kDa (~26x), while PEG300 kDa will fall below 1x, indicating that a 35-200 kDa sweet spot facilitates productive routing. Consistent with our observation that optimal-MW PEGs show minimal basolateral signal in the first 48 h followed by sharp acceleration, temporal kinetics are projected to concentrate informative transport within the 72-96 h window. Beyond PEG optimization, we expect the systematic coating library to reveal how charge density, biological recognition motifs, and hydrophobicity gradients independently modulate the balance between cellular retention and productive transcytosis. These outcomes will quantitatively link coating properties, intracellular trafficking pathways, and epithelial transport efficiency, establishing design rules for predictive NP engineering.

Potential Pitfalls and Alternative Strategies: If FTSC labeling reduces transport efficiency compared to unlabeled mucin controls, we will explore alternative approaches including secondary non-covalent fluorescent probes (e.g., lectin-based tags) to validate mucin distribution without modifying particle behavior. ImageJ thresholding may fail to discriminate closely apposed fluorescence signals; to mitigate this, we will correlate area-based quantification with spectrophotometric analysis of extracted basolateral fluorescence. Live/dead viability assays will be performed at each collection timepoint (24, 48, 72, and 96 h) to verify that monolayer integrity and cell health are maintained throughout the experiment; only wells retaining ≥95% viability will be included in transcytosis analyses. Our preliminary experiments confirm that untreated and NP-treated Caco-2 monolayers consistently meet this threshold at 96 hours. If any coating compromises cell viability, NP concentration will be reduced or incubation shortened (e.g., analyze at 72 h). To address TEM’s limited throughput while maintaining ultrastructural validation, we will implement correlative light–electron microscopy (CLEM) to improve confidence in subcellular localization and

## Aim 2: In-Vitro Model for Predicting NP Diffusion in Mucin.

Mucus diffusion is the first stage in the GI transport cascade, yet it is almost always studied in isolation from the epithelial and systemic stages that determine therapeutic outcome. The objective of this aim is to investigate how surface coatings — specifically mucin and polyethylene glycol (PEG) at varying molecular weights — govern nanoparticle diffusion through intestinal mucus, and to determine whether diffusion performance predicts the epithelial transport and systemic uptake measured in Aims 1 and 3. Using an in vitro, lumen-mimicking platform that enables rapid, high-throughput analysis [26, 27], we will measure particle size and zeta potential by dynamic light scattering (DLS) and calculate diffusion coefficients by confocal microscopy and NanotrackJ/ImageJ [28].

However, diffusion performance alone cannot be assumed to predict delivery. Our Aim 1 data reveal a striking disconnect between sequential transport stages: coatings that maximize cellular internalization do not maximize transcytosis (the B(+/−) paradox), demonstrating that success at one stage of GI transit does not guarantee success at the next. If this disconnect exists between cellular uptake and transcytosis, there is no basis for assuming that mucus diffusion — an even earlier stage — reliably predicts systemic outcome. This motivates a systematic evaluation of whether, and under what conditions, mucus transport metrics correlate with the downstream indices measured in Aims 1 and 3.

The broader literature on surface charge and mucin interactions compounds this uncertainty. Negatively charged and hydrophilic NPs reportedly show minimal mucin interactions, while positively charged and hydrophobic NPs interact strongly [19] — yet mucin coating of negatively charged gold NPs increased their endocytosis by 250% [23]. Enhanced uptake has been reported for both positively [38-40] and negatively charged NPs [41-43], and mucin itself has been shown to both adhere to PEGylated particles and impede their movement [23]. Alternative stealth coatings, including zwitterionic polymers [29] and poly(2-oxazoline) coronas [30], are under investigation but lack comprehensive oral bioavailability data, making them candidates for future extension of this framework. The recognition that anti-PEG antibodies form after repeat dosing [27] further narrows the field’s options. Our hypothesis offers a unifying explanation for these contradictions: mucus and mucus-like substances coat charged particles, neutralizing their surface charge and increasing their diffusion coefficients [14, 15, 26], with the extent of this biocoating varying by polymer type — as our data show that mucosal coating reduces particle zeta potential to nearly match that of the GI lumen [14, 15]. Testing this hypothesis systematically, across coating types and molecular weights, is the central objective of this aim.

The rationale for a systematic mucus mobility investigation stem from a critical gap exposed by the PEG literature. PEG coatings are the most widely used strategy for enhancing nanoparticle mucus penetration, yet the assumption that improved mucus transport translates to higher systemic uptake of intact particles is not supported by the most rigorous quantitative studies [57, 59]. An AUC-based bioavailability comparison of PEG-coated gold nanoparticles in rats found that absolute oral bioavailability remained below 0.1% for all PEG molecular weights tested, even when the oral dose was 10-fold higher than the intravenous dose [58]. Meanwhile, PEG chain length and surface density impose competing constraints: insufficient coverage increases adhesive trapping in mucus, while longer chains can hinder penetration through entanglement, and repeated PEG exposure can elicit anti-PEG antibodies that accelerate clearance [59, 60]. These findings demonstrate that mucus penetration is necessary but not sufficient for systemic delivery, and that PEGylation alone cannot be assumed to solve the oral absorption problem.

This “PEG dilemma” motivates the central design of Aim 2: rather than defaulting to a single PEG molecular weight as the benchmark, we will systematically evaluate mucin and PEG across a range of molecular weights, measuring not only diffusion rates but also mucus interaction states (free diffusion, reversible binding, irreversible trapping) to build a comprehensive mobility matrix. By pairing this matrix with the transcytosis data from Aim 1, we can identify coatings that optimize both mucus transit and epithelial transport — the combination that the PEG literature shows cannot be assumed from mucus data alone.

The predictive value of this approach is already supported by our preliminary data: mucin-coated polystyrene nanoparticles tested in the Caco-2 Transwell system (Aim 1) produce transport rankings that correspond to their systemic uptake in vivo, demonstrating that the in vitro platform can identify coatings with genuine oral bioavailability potential. Extending this analysis across a systematic PEG molecular weight series (Aim 2) will determine whether mucus mobility data further sharpen that prediction.

Based on these considerations, Aim 2 will systematically evaluate the mucus diffusion behavior of two core particle systems — fluorescent polystyrene (PS, labeled with PCRed for non-leaching tracking) and poly(lactic acid) (PLA) nanoparticles — at three sizes (450 nm, 1000 nm, and 2000 nm), coated with either mucin or PEG spanning a range of molecular weights (1.5–300 kDa). For each formulation, we will measure size, zeta potential, and diffusion coefficients in mucin gels, and classify each particle–coating combination into one of three interaction states: free diffusion, reversible binding, or irreversible trapping. This mobility matrix, integrated with the transcytosis data from Aim 1, will identify coating conditions that optimize both mucus transit and epithelial transport — enabling mechanism-guided selection rather than empirical screening.

Preliminary Data: We hypothesized that some polymeric NPs, with high bioadhesion, are capable of being coated with mucin, and that this coating reduces the zeta potentials of said particles to near neutral [14, 15]. In addition to the change in surface charge, coated particles exhibit different hydrodynamic diameters, with particles over 2 microns exhibiting slower diffusion coefficients. To test this, we coated several different polymers (PBMAD, PS, PMMA, PLGA 50:50, PLGA 65:35, PLA, PLGA-Ester, PFASA, PEG-PLGA) in 0.1% mucin and measured their hydrodynamic diameter (volumetric average) and zeta potential in 0.1% mucin vs. water (Figures 2 and 3) [14, 15]. Figure 2 shows a notable increase in hydrodynamic diameter for most polymeric NPs in mucin solution compared to deionized (DI) water. Since these polymers — with the exception of PEG-PLGA — are not prone to swelling in aqueous solutions, the observed diameter change indicates mucin biocoating. PBMAD NPs showed the most pronounced size increase (threefold), while P(FA:SA) 20:80 and PEG-PLGA (50:50) showed no statistically significant change. The stability of PEG-PLGA is likely attributable to PEG’s hydrophilic interface, which mitigates surface interaction with mucin [31]; the unchanged diameter of P(FA:SA) 20:80 may reflect its rapid hydrolysis in water [44].

Figure 3 shows that all tested polymers exhibited a negative surface charge in DI water, spanning from −17 to −53 mV. In 0.1% mucin solution, however, their charge diminished significantly to a range of −7.7 to −16 mV — closely matching the −7.3 mV charge of neat 0.1% mucin. This convergence suggests that mucin biocoating effectively masks the inherent charge of the polymers, shifting them toward neutrality. No correlation was observed between the size increase and the corresponding charge reduction, indicating that these are independent consequences of mucin adsorption. The mucin-induced size change was even more pronounced for positively charged silica NPs, with diameter increasing from 40 to nearly 1000 nm [19, 45], confirming that mucin interacts with NPs across a range of charges and hydrophobicities. These findings, corroborated by other studies [46], are consistent with our TEM observations of mucus-biocoated NPs in the GI tract [14, 15] — specifically, PLA8 microparticles loaded with colloidal gold and antibody, showing mucin strands attached to the particle surface [14, 15].

To determine whether mucin biocoating also affects NP mobility in mucus, we measured the mucosal diffusion coefficient (Dm) and propensity for cluster formation across four polymer types selected to span a range of mucin interaction strengths: PCR-PS and PS 125–250 kDa NPs (hydrophobic interactions), PLA8 NPs (electrostatic interactions), and PMMA NPs (minimal interactions). NPs were dispersed in either DI water (uncoated) or 0.1% mucin solution (biocoated) and then introduced into a 5% mucin gel simulating mucosal barrier composition [47]. The resulting diffusion coefficients are summarized in Table 1.

Table  - In vitro diffusion coefficient (Dm) of mucin biocoated and uncoated PMMA, PCRPS, PS 125–250 kDa, and PLA8 polymeric NPs in a 5% mucous gel.

| Polymer type | Dm in 5% mucin uncoated (cm2 s−1) | Dm in 5% mucin, biocoated with 0.1% Mucins (cm2 s−1) | Gain [folds] |
| --- | --- | --- | --- |
| PMMA | (1.9 ± 0.2) × 10−10 | (1.8 ± 0.2) × 10−10 | 0.9 |
| PCRPS | (6.8 ± 2.9) × 10−08 | (8.8 ± 3.4) × 10−08 | 1.3 |
| PS 125–250 | (2.2 ± 0.5) × 10−08 | (1.1 ± 0.4) × 10−07 | 5.2 |
| PLA8 | (3.4 ± 1.5) × 10−08 | (7.3 ± 0.1) × 10−07 | 21.3 |

Mucin biocoating produced polymer-dependent changes in diffusion. PCRPS NPs showed a modest 1.3-fold increase in Dm, while PS 125–250 NPs demonstrated a more substantial 5.2-fold enhancement. PMMA NPs were unaffected by biocoating. The most dramatic change was observed for PLA8 NPs, which exhibited a 21.3-fold increase in Dm. Notably, PLA8 and PS 125–250 NPs — both carrying high surface charges in water that were reduced by mucin biocoating — showed the highest diffusion rates, suggesting that mucin biocoating primarily enhances the mobility of charged NPs. Cluster analysis revealed that biocoated PLA8 NPs formed 20% fewer aggregates in 5% mucin compared to uncoated NPs, while biocoated PCRPS NPs exhibited a 20% increase in aggregation. PS 125–250 and PMMA NPs showed no change in cluster formation. These findings underscore the importance of assessing NP properties in the presence of mucin.

## Research Design:

Activity 2.1 – NP Manufacturing: Mucin from porcine stomach Type II will be used for both coating and GI lumen simulation, as it best mimics intestinal mucin without adding variability. Two core particle systems will be prepared at three sizes (450 nm, 1000 nm, and 2000 nm): fluorescent polystyrene (PS) incorporating PCRed particles for non-leaching confocal tracking, and poly(lactic acid) (PLA) as the biodegradable counterpart. PS NPs will be synthesized by established solvent evaporation [54] and PLA NPs by nanoprecipitation [53] methods. PCRed PS particles are incorporated into the polymer solution during synthesis at a 1:100 ratio so that NP surface characteristics originate from the non-PCRed polymer; embedding PCRed PS rather than free dye prevents leaching and improves detection efficiency. Each particle system will be coated with either mucin or PEG spanning molecular weights from 1.5 to 300 kDa. Particle charge (zeta potential), size, and shape (SEM and TEM) will be characterized before and after coating. An effective enhancement of diffusion will be defined as at least a 2-fold increase in the diffusion coefficient of coated particles compared to uncoated controls.

Activity 2.1 – NP Manufacturing: We will use mucin from porcine stomach Type II to simulate both the GI lumen environment and the coating procedure, as it best mimics intestinal mucin without adding variability. Two core particle systems will be prepared at three sizes (450 nm, 1000 nm, and 2000 nm): fluorescent polystyrene (PS) incorporating PCRed particles for non-leaching confocal tracking, and poly(lactic acid) (PLA) as the biodegradable counterpart. PS NPs will be synthesized by the solvent evaporation (SE) method [54]: PS is dissolved in DCM with Span-80, added to a polyvinyl alcohol (PVA) and 1-octanol solution, and collected via centrifugation. PLA NPs will be prepared by the precipitation with a non-solvent (PIN) method [53]: polymer is dissolved in DCM with or without colloidal gold and added to hexane or petroleum ether at a 1:100 ratio, with NPs collected on a hydrophobic PTFE filter. For confocal-based diffusion measurements, PCRed PS particles are incorporated into the polymer–DCM solution during the PIN step at a 1:100 ratio, ensuring that the surface characteristics of the NP originate from the non-PCRed polymer. Using PCRed PS instead of pure dye prevents dye leaching and incorporates the fluorescent label within the NP matrix, resulting in higher detection efficiency. Each particle system will be coated with either mucin or PEG spanning molecular weights from 1.5 to 300 kDa. Particle charge (zeta potential), size, and shape (SEM and TEM) will be characterized before and after coating. An effective enhancement of diffusion will be defined as at least a 2-fold increase in the diffusion coefficient of coated particles compared to uncoated controls.

Activity 2.3 – Diffusion and Cluster Measurements: NPs with incorporated PCRed PS will be divided into uncoated controls and particles coated in mucin solutions of 0.001%, 0.01%, and 0.1%. Samples will be prepared by placing mucin gels (3% or 5%) into an iSpacer chamber on a glass slide, followed by 5 µL of NP suspension; the thin well geometry ensures low Z-axis variance and reduces tracking noise. Slides will be scanned at multiple locations using a Nikon Ti2-E Widefield Fluorescence Microscope, and the interval between preparation and scanning will be recorded, as aggregation and settlement may affect measured diffusion coefficients. NP movement will be tracked at 0, 15, 30, and 60 minutes after immersion to determine whether mucin viscosity and particle mobility shift over the experimental window. Diffusion coefficients will be calculated with the NanoTrackJ plugin for ImageJ; cluster analysis will be performed separately using ImageJ's Particle Analysis function, with clusters defined as aggregates exceeding a minimum particle count. Diffusion coefficients and cluster sizes will be assessed across mucin concentrations, NP types, coating conditions, and time intervals using regression and mixed models to account for correlations in repeated measurements. The significance level will be set at α = 0.05, with non-parametric alternatives or transformations applied if assumptions are violated.

Activity 2.3 – Diffusion and Cluster Measurements: To prepare samples for confocal imaging, an iSpacer chamber will be placed on a glass slide, creating a thin well that ensures low Z-axis variance and reduces noise during particle tracking. Once PCRed PS particles are incorporated into NPs, some will be reserved as uncoated controls while others will be coated in mucin solutions of 0.001%, 0.01%, and 0.1%. Mucin gels of 3% or 5% will then be added to the chamber, followed by 5 µL of prepared NPs. Slides will be covered and scanned at multiple locations using a Nikon Ti2-E Widefield Fluorescence Microscope. Time between sample preparation and scanning will be recorded, as it may affect diffusion coefficients through aggregation, settlement, and reduction in free energy within the system. We will track NP movement at 0, 15, 30, and 60 minutes after immersion in mucin gel; time-course measurements will indicate whether mucin viscosity and NP mobility change over the experimental window. Captured time-lapse images will undergo contrast enhancement, smoothing, sharpening, and binary conversion for ImageJ analysis. Clusters will be defined as particle aggregates containing a minimum number of particles. Diffusion coefficients will be calculated using the NanoTrackJ plugin for ImageJ; cluster analysis will use ImageJ’s Particle Analysis function. Diffusion coefficients and cluster sizes will be assessed across mucin concentrations, NP types, coating conditions, and time intervals. Regression models — including mixed models to account for correlations in repeated measurements — will evaluate the impact of each factor and their interactions. The significance level will be set at α = 0.05; assumptions of all statistical tests will be verified, with non-parametric alternatives or transformations applied if violated.

Expected Outcomes: We anticipate that mucin and mid-range PEG coatings (35–200 kDa) will produce the largest increases in diffusion coefficients, consistent with the transcytosis optimum identified in Aim 1. Specifically, we expect mucin-biocoated PS and PLA NPs to show ≥5-fold increases in Dm relative to uncoated controls, with the magnitude of enhancement depending on the native surface charge of the core particle, as demonstrated by the 21.3-fold gain for PLA8 in our preliminary data. PEG coatings are expected to show a molecular-weight-dependent diffusion profile, with shorter chains (≤10 kDa) providing insufficient mucus shielding and longer chains beginning to impede penetration at ≥300 kDa, where our Aim 1 data show transcytosis efficiency drops sharply (0.64x ratio for PEG300k vs. 25.56x for PEG35k), likely reflecting entanglement effects in the mucus mesh. PEG molecular weights up to 200 kDa are expected to retain productive diffusion, consistent with the observation that transcytosis remains active across this range. The resulting diffusion–interaction matrix, integrated with Aim 1’s transcytosis indices, will identify formulations that optimize both mucus transit and epithelial transport, providing the quantitative input for Aim 3’s in vivo validation.

Potential Pitfalls and Alternative Strategies: Confocal microscopy may impose limitations on particle tracking, including restricted tracking speed and confinement to a single 2D focal plane, reducing the number of frames in which a particle remains in focus. To mitigate this, we will acquire a dedicated Particle Tracker for diffusion coefficient measurements, providing more comprehensive and accurate 3D tracking data. In addition, a ZetaView instrument will enable diffusion coefficient determination even for unlabeled samples, expanding the range of formulations we can characterize without requiring fluorescent incorporation.

# AIM 3: Impact of Biocoating on NP Absorption and Systemic Uptake via Isolated Loop

Introduction: This aim validates whether in vitro transcytosis indices (Aim 1) and mucus diffusion coefficients (Aim 2) predict actual systemic uptake in vivo. We employ two complementary models: the isolated intestinal loop (IL), which controls dose, contact time, and mucosal environment for quantitative mapping to in vitro data, and oral gavage, which subjects top-performing formulations to full GI transit. The same particle systems from Aims 1 and 2 (PS/PCRed and PLA NPs at 450 nm and 1000 nm with mucin or PEG coatings at varying molecular weights) will be tested under three IL conditions: (i) pre-coated NPs with native mucus intact, (ii) uncoated NPs for spontaneous corona formation, and (iii) coated and uncoated NPs in mucus-free loops. This design directly tests whether the mucus interaction parameters from Aim 2 predict in vivo performance and whether spontaneous corona formation in native mucus differs from pre-applied coatings. Plasma AUC and organ biodistribution will be mapped back to Aim 1/Aim 2 indices as absolute bioavailability values, the central deliverable of this grant. Our preliminary data support this approach: PS NPs achieved 45% systemic uptake via IL and 35% via oral gavage [14, 16], PLA8 reached ~30% [14, 15], and NP-encapsulated vedolizumab achieved 73% bioavailability relative to SubQ injection in a pilot IL study.

Preliminary Results: Detection and Quantification of NPs in the Bloodstream. Our lab's decade of in vivo work established that NPs must rapidly traverse the mucosal layer to outpace GI clearance and reach systemic circulation [14, 17, 35, 55, 56]. Bioadhesive coatings dramatically improve this transit: PMMA NPs coated with PBMAD increased systemic uptake from 6% to 66% [16], and bioadhesive encapsulation enhanced bioavailability of insulin and dicumarol [17, 32-37, 56]. With polystyrene particles, systemic uptake reached 45% via isolated loop and 35% after oral gavage [14, 16]. Many bioadhesive NPs exhibited pronounced negative zeta potentials linked to abundant carboxylic groups. We demonstrated that mucin biocoating significantly enhances NP diffusion and reduces aggregate formation [14, 15]. While we did not establish a definitive correlation between bioadhesiveness and ZP in DI water or 0.1% mucin solution, we propose that optimal systemic uptake requires a robust negative ZP neutralized by mucin biocoating to enhance bioadhesion. Comparing polymer platforms, PS NPs showed superior uptake over PMMA [16], directing our focus to PLA8. Upon biocoating, PLA8 exhibited a significant ZP shift (-48 to -12 mV) and notable bioadhesive force (~1800 mN/cm2). Given its biodegradability and biocompatibility, PLA8 achieved ~30% bioavailability (35+/-6.9%) via FTIR detection [14, 15], with traces in liver, lungs, and spleen [14, 15].

Table  - Percent bioavailability from IL experiments for formulations F82 and F65N compared to the average bioavailability for IV and SQ administration in rat

| Rat | BA (%) relative to IV | BA (%) relative to SQ |
| --- | --- | --- |
| 1 (F82) | 3.7 | 86.8 |
| 2 (F82) | 2.0 | 47.0 |
| 3 (F65N) | 4.3 | 102.2 |
| 4 (F65N) | 2.4 | 56.6 |
| AVG BA | 3.08 | 73.2 |

Experimental Approach: Rationale: The isolated intestinal loop (IL) is the logical validation model for this framework because it recapitulates the full biological complexity of intestinal absorption (native mucus, intact epithelium, peristalsis, lamina propria clearance, live blood and lymphatic flow) while excluding the GI transit confounders detailed in Activity 3.2. Aims 1 and 2 deliberately isolate two variables: epithelial processing (Caco-2) and mucus diffusion (gel platform). Oral gavage would reintroduce confounders that make it impossible to determine whether systemic performance reflects coating-dependent transport or simply upper GI survival; the IL eliminates these while preserving the three-dimensional architecture of intact villi. Critically, the loop targets the jejunum, the same Peyer's patch-poor region where our preliminary data demonstrate that intact particle uptake occurs via an enterocyte-dominant pathway [14-16], so predictions from a Caco-2 (enterocyte) model are tested in the tissue compartment where they are most directly applicable. Because dose, mucosal surface area, and contact duration are precisely controlled, plasma AUC and organ biodistribution can be computed as absolute bioavailability values and mapped quantitatively back to the in vitro transcytosis index (Aim 1) and mucus mobility scores (Aim 2). The loop's surgical accessibility also enables a control unavailable in gavage: the luminal mucus environment can be manipulated (intact loose mucus vs. PBS-flushed) to test whether Aim 2 mucus interaction parameters predict in vivo performance and whether spontaneous corona formation in native mucus differs from pre-applied coatings [14, 15]. We will test the same particle systems described in Activity 2.1 under three loop conditions: (1) pre-coated NPs with native loose mucus intact, (2) uncoated NPs for spontaneous corona formation, and (3) coated and uncoated NPs in a PBS-flushed mucus-free loop. Blood samples will be analyzed via FTIR [14, 15] and SEC-MS, with an LOD of 10 ng/mL. Formulations that best validate the predictive framework will advance to oral gavage (Activity 3.2).

Methodology and Procedure: Sprague-Dawley rats (200-250 g; 50% male, 50% female), fasted for 24 hours, will undergo IL surgery following our established protocol [16]. Polymeric NPs (100 mg/mL in PBS) will be introduced into a 10 cm jejunal loop. Five hours post-injection, animals are euthanized and the IL segment is collected alongside liver, kidneys, and heart. The IL is rinsed with PBS and incised longitudinally to collect loose mucus for interaction studies; a neighboring intestinal section serves as control. Specimens are flash-frozen and lyophilized with dry mass recorded. Blood samples are centrifuged and serum stored at -80°C. NP detection proceeds via three complementary methods. FTIR quantifies polymer content in blood [14, 15]. SEC-MS provides independent quantification in blood and tissues (homogenized, lyophilized, chloroform-processed), achieving an LOD of 10 ng/mL. DESI-MSI (Waters Xevo TQ Absolute with DESI XS source) maps polymer-specific mass signatures spatially in unprocessed tissue sections, confirming intact NP localization within tissue architecture without homogenization or extraction. Statistical analysis implements ANOVA with significance set at p ≤ 0.05.

Methodology and Procedure: In vivo experiments will use the isolated loop (IL) approach as outlined in [16]. Sprague-Dawley rats (200–250 g; 50% male, 50% female), following a 24-hour fast, are anesthetized. The abdominal region is shaved and a sternum incision provides access to a 40 cm jejunum-ileum section near the cecum. Two knots are placed: a tight knot at one end, with a loose knot approximately 10 cm above it. Following this, 100 mg/mL of polymeric NPs in PBS is introduced into the loop, secured by the upper knot. Five hours post-injection, animals are euthanized and the IL segment is collected alongside critical organs — liver, kidneys, and heart. The IL is rinsed with PBS; a neighboring intestinal section is harvested as a control. The IL is incised longitudinally to isolate and collect loose mucus for interaction studies. Each specimen is flash-frozen, lyophilized, with dry mass recorded. Blood samples rest for 25 minutes at room temperature and undergo centrifugation at 4°C and 2000g for 18 minutes; separated serum is stored at −80°C. Detection and quantification of NPs proceed via FTIR [14, 15]. Polymer content in blood is additionally analyzed through size exclusion chromatography–mass spectrometry (SEC-MS), with tissues homogenized, flash-frozen, lyophilized, and chloroform-processed for purification prior to MS analysis, achieving an LOD of 10 ng/mL. In addition, tissue sections from the intestinal loop and systemic organs will be analyzed by desorption electrospray ionization mass spectrometry imaging (DESI-MSI) using a Waters Xevo TQ Absolute equipped with a DESI XS source, enabling direct spatial mapping of polymer-specific mass signatures in unprocessed tissue without homogenization or extraction. This approach confirms intact NP localization within the tissue architecture and eliminates the fluorescence-based confound of dye leaching from labeled particles. Statistical analysis implements ANOVA with significance set at p ≤ 0.05.

Activity 3.2 – Oral Gavage Confirmation of Top-Ranked Formulations: Following completion of the IL studies, the two to three formulations whose loop-derived systemic uptake is most accurately predicted by the combined Aim 1 transcytosis index and Aim 2 mucus mobility score will advance to oral gavage. This step subjects top-ranked formulations to the full GI transit pathway, including the gastric, enzymatic, and regional confounders that the IL deliberately excluded. Rats will be fasted overnight and receive a single oral dose by gavage. Animals will be followed for 5 days, with serial blood samples collected for plasma AUC determination and organs harvested at endpoint for biodistribution analysis, matching the IL readouts. The extended observation window captures delayed absorption, tissue accumulation, and clearance kinetics that the 5-hour loop cannot assess. Comparison of gavage-derived and loop-derived bioavailability for the same formulations directly tests whether the Aim 1/Aim 2 indices retain predictive power under full physiological complexity, or whether additional variables must be incorporated into future framework iterations. We estimate 24 additional rats (n = 8 per formulation, 3 formulations; 50% male/female).

Expected Outcomes: Formulations combining high transcytosis indices with high mucus diffusion coefficients are expected to produce the highest systemic bioavailability in the IL model. Based on our preliminary data, mucin-biocoated PS and PLA NPs should achieve ≥30% bioavailability through the isolated loop [14, 15, 16], with the magnitude of enhancement depending on the interplay between coating-mediated mucus transit (Aim 2) and epithelial processing efficiency (Aim 1). Comparing pre-coated vs. spontaneously coated NPs will reveal whether the biomolecular corona formed in native mucus replicates or diverges from laboratory-applied coatings, a key question for translational design. The mucus-free loop condition will quantify the isolated contribution of epithelial processing, allowing direct comparison with Aim 1 Caco-2 transcytosis data. Oral gavage results will test whether the Aim 1/Aim 2 indices retain accuracy under full GI transit or whether additional variables must be incorporated into future framework iterations. Together, these data will produce a validated mapping from in vitro indices to in vivo bioavailability.

Expected Outcomes: We anticipate that the formulations identified as top performers in Aims 1 and 2 — those combining high transcytosis indices with high mucus diffusion coefficients — will produce the highest systemic bioavailability in the IL model. Based on our preliminary data, mucin-biocoated PS and PLA NPs are expected to achieve ≥30% bioavailability through the isolated loop [14, 15, 16], with the magnitude of enhancement depending on the interplay between coating-mediated mucus transit (Aim 2) and epithelial processing efficiency (Aim 1). Comparing pre-coated vs. spontaneously coated NPs will reveal whether the biomolecular corona formed in native mucus replicates or diverges from laboratory-applied coatings — a critical question for translational design. The mucus-free loop condition will quantify the isolated contribution of epithelial processing alone, allowing direct comparison with Aim 1’s Caco-2 transcytosis data. Oral gavage results will test whether the Aim 1/Aim 2 predictive indices retain accuracy under full GI transit, or whether additional variables — gastric survival, bile salt exposure, regional transit variability — must be incorporated into future iterations of the framework. Together, these data will produce a validated mapping from in vitro indices to in vivo bioavailability, the central deliverable of this grant.

Potential Pitfalls and Alternative Strategies: Variability in IL bioavailability between animals may arise from differences in mucus thickness, vascular perfusion, or surgical preparation. We mitigate this with balanced sex ratios (3M/3F per group), standardized surgical technique, and the inclusion of paired controls from neighboring intestinal segments. If FTIR sensitivity proves insufficient for low-uptake formulations, SEC-MS provides a complementary quantification route with an LOD of 10 ng/mL, and DESI-MSI of tissue sections will provide spatial confirmation of intact NP presence via polymer-specific mass signatures. For oral gavage, gastric degradation of PLA NPs could reduce detectable systemic uptake; we will include enteric-coated capsules as an alternative delivery vehicle if initial gavage results show excessive NP degradation before intestinal contact.

Statistical Analysis: Bioavailability differences between coated and uncoated NPs will be analyzed using one-way ANOVA with post-hoc Tukey’s HSD, with significance set at α = 0.05. Power analysis confirms that n = 6 per group provides ≥88% power to detect large effects (Cohen’s d ≥ 2.0), consistent with preliminary effect sizes (coated vs. uncoated: d ≈ 2–3). For subtler comparisons between coating types (estimated d ≈ 1.0), n = 6 provides 35% power; these comparisons will be treated as exploratory and hypothesis-generating. Regression models will map in vivo bioavailability to Aim 1 transcytosis indices and Aim 2 diffusion coefficients to assess the predictive accuracy of the integrated framework.

Animal Procedures: Sprague-Dawley rats (200–250 g; 50% male, 50% female) will be used for all in vivo work. Activity 3.1 tests 4 particle formulations (PS/PCRed and PLA at 450 nm and 1000 nm) × 4 coating conditions (uncoated plus three top-performing coatings from Aims 1 and 2) × 2 mucus conditions (native mucus intact vs. PBS-flushed), for 32 experimental groups plus 4 loop controls (no particles), totaling 36 groups × 6 rats = 216 rats. Activity 3.2 tests 3 top-ranked formulations by oral gavage at n = 8 per formulation (24 rats). Combined Aim 3 animal use is 240 rats over 5 years. All procedures conform to the Animal Welfare Act, NIH Guide, federal/state regulations, and Brown University IACUC policies.

Timeline: In Year 1, we will synthesize and characterize NP formulations, establishing quality control protocols and initiating Caco-2 transcytosis studies (Aim 1) and in vitro diffusion measurements (Aim 2). Year 2 will complete cellular uptake studies, correlate transcytosis indices with coating properties, and finish the mucus diffusion matrix. Year 3 will focus on isolated loop experiments (Aim 3, Activity 3.1), beginning with PS/PCRed formulations and expanding to PLA NPs. Year 4 will complete IL studies across all formulations and mucus conditions, integrate in vitro and in vivo data to validate the predictive framework, and advance top formulations to oral gavage (Activity 3.2). Year 5 will finalize gavage studies, complete the predictive model validation.

References:

EQUIPMENT JUSTIFICATION — WATERS XEVO TQ ABSOLUTE WITH DESI XS IMAGING SOURCE

Waters Xevo TQ Absolute with DESI XS Imaging Source (to be placed by Waters Corporation). This triple quadrupole mass spectrometer equipped with a Desorption Electrospray Ionization (DESI XS) source enables direct molecular imaging of tissue sections without homogenization, extraction, or chemical processing — a tissue section is placed on a glass slide and analyzed directly. The DESI XS sprays charged solvent microdroplets onto the tissue surface, desorbing and ionizing molecular species that are then detected with the high sensitivity and selectivity of multiple reaction monitoring (MRM) on the Xevo TQ Absolute.

This instrument is essential to the proposed research for three reasons. First, it provides unambiguous confirmation of intact nanoparticle presence in tissue by detecting polymer-specific mass signatures — polystyrene and poly(lactic acid) fragment ions — rather than relying on fluorescent labels that can dissociate from the particle through dye leaching, a recognized confound in oral NP uptake studies. Second, DESI imaging preserves spatial information: rather than reporting bulk polymer concentration in a tissue homogenate, we can map exactly where nanoparticles localize within the intestinal wall (mucus layer, enterocyte cytoplasm, lamina propria, vascular/lymphatic channels) and in systemic organs (liver sinusoids, splenic red pulp, renal cortex), directly testing the enterocyte-mediated transcytosis pathway central to this proposal. Third, the same analytical capability applies to detecting environmental micro- and nanoplastic accumulation in tissue — the instrument acquired for Aim 3 validation becomes a platform for the broader public health question of how ingested plastic particles reach systemic organs.

No equivalent capability currently exists at Brown University. Existing FTIR-based detection [14, 15] provides bulk quantification but no spatial resolution, and SEC-MS requires tissue homogenization and solvent extraction, destroying anatomical context. The DESI XS–Xevo TQ Absolute system fills both gaps simultaneously: spatial mapping with quantitative sensitivity (LOD in low ng/mL range), directly from unprocessed tissue.